MATERJALI OMADUSED

Omadused Tulemused Testi meetod Tõmbetugevus 6,000 psi ASTM D 638 Tõmbemoodul 600,000 psi ASTM D 638 Paindetugevus 10,000 psi ASTM D 790 Paindepiir 1,000,000 psi ASTM D 790 Pikenemine 0.5% ASTM D 638 Kõvadus 92 Rockwell "M" skaala 65 Barcol Impressor ASTM D 785 ASTM D 2583 Soojuspaisumine 2.0 x 10-5 in/in F˚ ASTM D 696 Läige (60 Gardner) 5 – 20 vahel NEMA LD-3 Värvistabiilsus 200 tunni jooksul muutust ei toimunud NEMA LD-3 Määrdumisvastupidavus Läbitud Nimiväärtus 41 ANSI Z 124 Hõõrdevastupidavus Läbitud ANSI Z 124 Tasapinna vastupidavus keevale veele Mõju ei ole NEMA LD-3 Vastupidavus kõrgele temperatuurile Mõju ei ole NEMA LD-3 IZOD löögikindlus (sälkmeetod) 0.28 ft.lbf/in ASTM D 256 Ball drop 12.3 mm leht 144" w/ 1/2 lb ball, purunemiseta NEMA LD-3 Bakteritele ning seentele vastupidavus Kasvu ei ole ASTM G 21, G22 Suhteline tihedus Ühevärviline Mustriline 1.72 1.69 ASTM D 792 Niiskumine 0.04%, (12,3 mm- 24 tundi) 0.11%, (3 mm- 24 tundi) ASTM D 570 Süttivus Leegi levik Suitsu tihedus Klass A / Klass 1 10 10 UBC 8-1 ASTM E 84 ASTM E 84 Vastupidavus kiirgussoojusele Märgatavat mõju ei ole NEMA LD-3 Toksilisus 84.4g (Ühevärviline) 81.8g (Mustriline) Pittsburgh Test Protocol (LC50 Test)

PROPERTIES TYPICAL RESULTS TEST PROCEDURE Tensile strength 6,000 psi ASTM D 638 Tensile modulus 600,000 psi ASTM D 638 Flexural strength 10,000 psi ASTM D 790 Flexural modulus 1,000,000 psi ASTM D 790 Elongation 0.5% ASTM D 638 Hardness 92 Rockwell "M" Scale 65 Barcol Impressor ASTM D 785 ASTM D 2583 Thermal expansion 2.0 x 10-5 in/in F˚ ASTM D 696 Gloss (60 Gardner) Between 5 - 20 NEMA LD-3 Color stability No change-200hrs NEMA LD-3 Stain resistance Pass Rating 41 ANSI Z 124 Abrasion resistance Pass ANSI Z 124 Boiling water surface resistance No effect NEMA LD-3 High temperature resistance No effect NEMA LD-3 IZOD Impact resistance (notched) 0.28 ft.lbf/in ASTM D 256 Ball drop 1/2"(12.3 mm) sheet 144" w/ 1/2 lb ball, No failure NEMA LD-3 Fungi and Bacterial resistance No growth ASTM G 21, G22 Specific gravity Solid colors Patterened colors 1.72 1.69 ASTM D 792 Water absorption 0.04%, (1/2", 24hrs) 0.11%, (1/8", 24hrs) ASTM D 570 Flammability Flame spread Smoke density Class A / Class 1 10 10 UBC 8-1 ASTM E 84 ASTM E 84 Radiant heat resistance No visual effect NEMA LD-3 Toxicity 84.4g (Solid Color) 81.8g (Patterned Color) Pittsburgh Test Protocol (LC50 Test) PERFORMANCE PROPERTIES

# Footnotes

Psi – naela ruuttollile ehk siin 41 368 543.8 paskalit

4.13685438 × 109 paskalit

68 947 572.9 paskalit

6.89475729 × 109 paskalit